# Properties of POBCO Materials

| ENGINEERING DATA | POBCO-B HARDWOOD | UHMW | LUBE-FILLED UHMW PLUS® | REPRO UHMW | (7) HI-TEMP. UHMW | (13) HI-WEAR UHMW | DRYWEAR UHMW | (11) NYWEAR | NYLON | (10) NYLON MD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CODE LETTERS | B | U | P | UR | UH | CP | DW | NW | N | MD |
| P.V. Cap psi-fpm (1) | 12,000 | 2,000 | 12,000 | 2,000 | 2,000 | 2,300 | 4,000 | 16,000 | 2,500 | 3,500 |
| Max. Surface Speed fpm | 500 | 100 | 300+ | 100 | 100 | 100 | 150 | 150 | 100 | 150 |
| Static Load Cap. psi | 1,000 | 1,000 | 600 | 900 | 1,000 | 1,000 | 1,000 | 1,000 | 1,000 | 1,000 |
| Service Temp. Range (2) oF | 180 | 180 | 165 | 180 | 275 | 200 | 180 | 230+ | 220 | 220 |
| Coef. of Friction Ave. | .09 | .15-.20 | .06-.12 | .15-.20 | .15-.20 | .16-.18 | .15 | .15 | .19 | .17 |
| Abrasion Resistance (3) | 1-3 | 1-2 | 1-2 | 1-2 | 1-2 | 1 | 1-2 | 3 | 3 | 3 |
| Dim. Stability in Water | Fair | Exc. | Exc. | Exc. | Exc. | Exc. | Exc. | Good | Fair | Fair |
| USDA/FDA Compliant | Indirect | yes | yes | no | yes | no | no | yes* | yes | no |
| Chemical Resistance at 73o F* |  |  |  |  |  |  |  |  |  |  |
| Acid Weak | A | A | A | A | A | A | A | A | A | A |
| Acid Strong | L | L | L | L | L | A | L | U | U | U |
| Alkalies Weak | A | A | A | A | A | A | A | A | A | A |
| Alkalies Strong | L | A | A | A | A | A | A | A | A | A |
| Hydrocarbon Aromatic | - | L | L | L | L | A | L | A | A | A |
| Hydrocarbon Aliphatic | - | A | A | A | A | A | A | A | A | A |
| Ketones | - | A | A | A | A | A | A | A | A | A |
| Ethers | - | A | A | A | A | A | A | A | A | A |
| Alcohols | - | A | A | A | A | A | A | A | A | A |
| Inorganic Salt Solution | A | A | A | A | A | A | A | A | - | A |
| Continuous Sunlight | A | U** | L | L | L | A | L | L | L | L |
| Standard Color | Brown | White | Grey/Brown | Black/Green | White | Black/Green | Black | Natural | White/Grey | Black |
| Low Temp oF* | - | -200 | - | -200 | - | - |  | -10 | -10 | -10 |

| ENGINEERING DATA | ACETAL DELRIN® | (8) ACETAL AF | VIRGIN PTFE | GLASS FILLED PTFE | POBLON | RULON® 641 | RULON® LR BEARING GRADE | ERTALYTE® | UNFILLED PEEK |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CODE LETTERS | D | DT | T | GT | TM | RF | RB | YT | PK |
| P.V. Cap psi-fpm (1) | 2,000 | 8,000 | 1,000 | 10,000 | 10,000 | 10,000 | 10,000 | 2,800 | 14,000 |
| Max. Surface Speed fpm | 100 | 150 | 100 | 400 | 400 | 400 | 400 | 125 | 100 |
| Static Load Cap. psi | 2,000 | 2,000 | 400 | 800 | 1,000 | 1,000 | 1,000 | 2,000 | 6,000 |
| Service Temp. Range (2)oF | 180 | 200 | 450 | 500 | 500 | 550 | 550 | 210 | 480 |
| Coef. of Friction Ave. | .22 | .08-.14 | .06-.15 | .10-.13 | .10-.30 | .10-.30 | .15-.25 | .20 | .20 |
| Abrasion Resistance (3) | 5 | 1-2 | 5 | 1-2 | 1-2 | 1-2 | 1-2 | 3 | 1-2 |
| Dim. Stability in Water | Good | Good | Exc. | Exc. | Exc. | Exc. | Exc. | Good | Exc. |
| USDA/FDA Compliant | yes | maybe | yes | no | Yes | yes | no | yes | yes |
| Chemical Resistance at 73o F* |  |  |  |  |  |  |  |  |  |
| Acid Weak | A | S | A | A | A | A | A | A | A |
| Acid Strong | U | U | A | A | A | A | A | L | L |
| Alkalies Weak | A | A | A | A | A | A | A | A | A |
| Alkalies Strong | U | U | A | A | A | A | A | U | A |
| Hydrocarbon Aromatic | A | A | A | A | A | A | A | A | A |
| Hydrocarbon Aliphatic | A | A | A | A | A | A | A | A | A |
| Ketones | A | A | A | A | A | A | A | L | A |
| Ethers | A | A | A | A | A | A | A | A | A |
| Alcohols | A | A | A | A | A | A | A | A | A |
| Inorganic Salt Solution | - | A | A | A | A | A | A | A | A |
| Continuous Sunlight | U | L | A | A | A | A | A | A | - |
| Standard Color | White | Brown | White | White | White | White | Maroon | White | Beige |
| Low Temp oF* | -40 | -40 | -200 | -200 | -400 | -200 | -200 | - | - |

*For Plastics – Dry Clearance is Standard

#1 At Room Temperature #2 At Low PV Levels

#3 Rating 1 (Excellent) to 5 (Fair)

#5 A=Acceptable L=Limited U=Unacceptable

#7 Thermal Expansion Is Up To 25% Less Than Normal UHMW with extended wear life

#8 PTFE-Filled Acetal

#10 Moly-Filled Nylon

#11 Lube-Filled Nylon - Bearing Grade Green, FDA Compliant Off White

#12 Green & Black Reprocessed UHMW

#13 33% More Wear Resistant than unfilled UHMW