# Wood Engineering Data

# POBCO-B Physical Properties (Lubricant-Filled Hardwood)

| Density (lbs/in3) | .038 | Tensile Strength | 1100 psi |
| --- | --- | --- | --- |
| Coefficient of Friction | .07-.112 | Permanent Deformation (7500 psi compression) | .005 set |
| Temperature Range | -50o to 180o | Coefficient of Thermal Expansion (per oF) | 4.3 x 10-6 |
| Specific Gravity | 1.2 | PV Factor (continuous duty) | 12,000 psi-fpm |
| Lubricant Content by Weight Load Weight (continuous duty) | 40% 1000 psi | Wear Rate Factor | <0.1x10-10 (inch) PV x hr. |

POBCO-B Bearings and Wear Strips

Our exclusive lubricant blend is impregnated into 100 percent of the hardwood, producing POBCO-B material from which the bearings & wear strips are manufactured. The lubricant on the bearing surface provides a low friction film for initial

start-up. During operation, additional lubricant is drawn to the bearing surface in a controlled flow to maintain a continuous film between the journal or chain and the bearing. The

flow constantly adjusts itself based on load, speed, and the requirements of the operation. When motion ceases, the bearing reabsorbs the lubricant. Reaming does not seal off the self- contained lubricants.

# POBCO-B is Nonconductive of Electric Current

POBCO B-Wood

POBCO B-Wood

3600

3450

3300

3150

3000

2850

2700

2550

2400

RPM of Shaft

RPM of Shaft

2250

2100

1950

1800

1650

1500

1350

1200

1050

900

750

600

450

300

150

0

0  25  50  75 100 125 150 175 200 225 250 275 300 325 350 375 400 425

Allowable Bearing Load in LBS per Inch of Bearing Length

# POBCO-B Bearing Lengths and Wall Thickness

Minimum bearing length and allowable bearing load per bearing are determined by using our bearing load curve. Since the lubricant blend is contained in the bearing wall, the thickness of the bearing wall should be equal to or greater than the

recommended minimum wall thickness, as shown on the chart. In most instances shaft diameters cannot be decreased. Frequently, however, the diameter of the bearing housing can be increased to obtain at least the recommended minimum bearing wall.

| POBCO-B SHAFT DIAMETER | RECOMMENDED MINIMUM WALL THICKNESS* |
| --- | --- |
| to 1/2” | 1/16”-1/8” |
| 1/2”-1” | 1/8”-3/16” |
| 1” to 1-1/2” | 3/16”-5/16” |
| 1-1/2” to 2” | 5/16”-3/8” |
| 2” to 2-1/2” | 3/8”-1/2” |
| 2-1/2” to 4” | 1/2”-5/8” |

*SATISFACTORY SERVICE CAN BE OBTAINED UNDER CERTAIN OPERATING CONDITIONS WITH WALL THICKNESS LESS THAN THOSE RECOMMENDED.

# Shaft Selection

To maximize the life of the bearing it is important to use proper shafting. Overall, steels with a finish of 16 RMS are the preferred choice. Hardened shafts should be used in abrasive applications. Common shaft materials include: carbon steels, stainless steels, hard chromed steels and hard anodized aluminums.

ENGINEERING FORMULAS

(For all materials)

Minimum Bearing Length = load/bearing x RPM

4 x PV Capacity

PV = load/bearing x RPM 4 x bearing length

ENGINEERING FORMULAS

(For all materials)

Minimum Bearing Length = load/bearing x RPM

4 x PV Capacity

PV = load/bearing x RPM 4 x bearing length